MECHANICAL BEHAVIOUR OF JUTE-GLASS FIBER REINFORCED HYBRID COMPOSITES

A Project Report Submitted To Jawaharlal Nehru Technological University

In Partial Fulfillment of Requirements for the Award of the Degree of

BACHELOR OF TECHNOLOGY

IN

MECHANICAL ENGINEERING

Submitted by

KORIVI RANGA NANDA KISHORE (09501A0323)

CHIPPALASESHI KOTESH (09501A0308)            KANNEGANTIGOWTHAM (09501A0320)

CHUKKAPALLI VINAY KUMAR (09501A0305)

Under The Esteemed Guidance Of

P .RAVI KUMARM.tech

ASSISTANT PROFESSOR

DEPARTMENT OF MECHANICAL ENGINEERING

PVPSIT, KANURU

DEPARTMENT OF MECHANICAL ENGINEERING

PRASAD.V.POTLURI SIDDHARTHA INSTITUTE OF TECHNOLOGY

(Accredited by NBA, an ISO 9001-2000 CERTIFIED INSTITUTION)

Affiliated to JNTU, Kakinada, Approved by AICTE, New Delhi

Kanuru, Vijayawada-520007

2009-2013

PRASAD.V.POTLURI SIDDHARTHA INSTITUTE OF TECHNOLOGY

(Accredited by NBA, an ISO 9001-2000 CERTIFIED INSTITUTION)

DEPARTMENT OF MECHANICAL ENGINEERING

CERTIFICATE

This is to certify that the project work titled “MECHANICAL BEHAVIOUR OF JUTE-GLASS FIBER REINFORCED HYBRID COMPOSITES” is a bonafide work done by

KORIVI RANGA NANDA KISHORE (09501A0323)

CHIPPALASESHI KOTESH (09501A0308)            KANNEGANTIGOWTHAM (09501A0320)

CHUKKAPALLI VINAY KUMAR (09501A0305)

Submitted in partial fulfillment of requirement for the award of degree of Bachelor of Technology in Mechanical Engineering during the year 2009 - 2013 by Jawaharlal Nehru Technological University.

P .RAVI KUMARM.tech                                                                      Dr.K.SIVAJI BABUP.hD             ASSISTANT PROFESSOR, Project Guide                                     HEAD OF THE DEPARTMENT

Department Of Mechanical Engineering                               Department Of Mechanical Engineering

PVPSIT, KANURU                                                                             PVPSIT, KANURU

ACKNOWLEDGEMENT

The satisfaction that accompanies the successful completion of any task would be incomplete without a mentioning the people, who made it possible and whose guidance and encouragement crown all the efforts with success.

We wish to place on record our profound gratitude to Dr.P.VenkateswarluP.hD, Principal, PVPSIT, Kanuru, Vijayawada for having given us the opportunity to complete this project successfully.

We reckon to a distant pleasure to endorse out indebtedness and deep sense of gratitude to  Dr.K.SIVAJI BABUP.hD, Head Of Department Of Mechanical Engineering for his encouragement in all endeavors.

We are greatly indebted to our project guide Sri.  P .RAVI KUMARM.tech, Assistant Professor, DEPARTMENT OF MECHANICAL ENGINEERING for his patience and cheerful readiness to help us in our project. We thank him for the support, encouragement, suggestions and co-operation during the course of the project.

We are also very much grateful to all the staff and faculty of the Department Of Mechanical Engineering for their cooperation during the course of this project work. Finally, we would like express our sincere thanks to Assistant Professor   M. Mounika for her helpful advices and constructive criticism during the course of this project work.

By

KORIVI RANGA NANDA KISHORE (09501A0323)

CHIPPALA SESHI KOTESH               (09501A0308)

KANNEGANTI GOWTHAM                (09501A0320)

CHUKKAPALLI VINAY KUMAR      (09501A0305)

ABSTRACT

Fiber reinforced polymer composites have a wide variety of applications as a class of structural materials because of their advantages such as ease of fabrication, relatively low cost of production & superior strength as compared to neat polymer resins. The fiber which serves as a reinforcement in polymers may be either synthetic or natural. Although, synthetic fibers such as glass, carbon etc.  possess high specific strength; their fields of applications are limited because of their higher costs of production.

Recently, there is an increasing interest in hybrid composites that are made by reinforcement of two or more different types of fibers in a single matrix, because these materials attain a range of properties that cannot be obtained with a particular kind of reinforcement. Further, material costs can be reduced by careful selection of reinforcing fibers. Currently, the trend is to produce hybrids of synthetic and natural fibers because this type of reinforcement in composites optimizes the production coast compared to those of synthetic fibers and also increases the structural properties of the composites compared to those of natural composites.

In this connection to this, an investigation has been carried out to make potential utilization of JUTE fiber as reinforcement with GLASS fiber in polyester polymer matrix which is very cheap and is easily available in India. The objective of the present research work is to study the effect of mechanical properties of jute and glass fiber composites individually by varying the volume fraction of fiber in the composites and compare them to the respective hybrids produced by varying the volume fraction of both fibers in the same matrix. The matrix used for current investigation is general purpose polyester resin. The specimens have been fabricated by hand-layup technique with different volume fraction of jute and glass fiber. Theoretically mechanical properties are predicted by rule of hybrid mixture model, using the resin and fiber properties together with their respective volume fraction and compared with the experimental results. Simulation is done using ANSYS software for tensile modulus to compare and conclude about the results obtained by the other methods.

CONTENTS

Chapter No:         Description                                                         Page No

Chapter 1                      INTRODUCTION                                                                               1- 20

1.1 Introduction to Composites                                                              2

1.2 Types of Fibers                                                                                 7

1.3 Hybrid Composites                                                                           13

1.4 Advantages of Composites	                                                     13

1.5 Introduction to ANSYS                                                                    16

1.6 Thesis Outline                                                                                   19

Chapter 2                       LITERATURE SURVEY                                                                   21-23

2.1. Literature review                                                                              22

2.2. The knowledge gap                                                                          22

2.3. Objectives of the present research work                                          23

2.4. Outline of research work                                                                  23

Chapter 3                       METHODS AND MEANS                                                                  24-41

3.1 Method for Theoretical Evaluation of                                              25

Mechanical Properties for Composites

3.2 Method for Evaluation of Actual                                                      30

Mechanical Properties for Composites

3.3 Method for Evaluation of Tensile Modulus                                      40

for Composites through Simulation

Chapter 4                        RESULTS AND DISCUSSION                                                          42-68

4.1. Behavior of Composites under Flexural Loading                           43

4.2. Behavior of Composites under Impact Loading	                   49

4.3. Behavior of Composites under Tensile Loading                             54

4.4. Behavior of Composites under In-Plane Shear Loading                 66

Chapter 5                        CONCLUSIONS                                                                                 69- 74

5.1 Conclusions Based on Behavior of Composites                             70

under Flexural Loading and Impact Loading

5.2 Conclusions based on behavior of composites                               71

under tensile loading

5.3 Conclusions based on behavior of composites                               73

under Shear loading

5.4 Scope for Future Work                                                                   74

REFERENCES                                                                                   75

LIST OF TABLES

Table No.                      Name                                                          Page No.

1.1                           Chemical Composition of Natural Fibers                                                        10

1.2                           Properties of Natural Fibers                                                                             12

3.1                           List of Formulas for Theoretical Evaluation of                                                30

Mechanical Behavior of Composites

3.2                           Test sample dimensions with respect to type of test                                        34

3.3                           Test sample composition in volume fraction                                                   34

4.1                           Loads and Corresponding Deflection obtained in Experimentation                43

Process for Three-Point Bending Test

4.2                           Stress, Strain and Young’s Modulus obtained in Experimentation                  44

Process for Three-Point Bending Test

4.3                          Energy Absorbed and Impact Strength obtained in                                          49

Experimentation Process (Izod impact testing)

4.4                          Young’s modulus (E1) and Poisson’s ratio (ϑ12) in                                         54

direction obtained by rules of mixture

4.5                         Young’s modulus (E2) and Poisson’s ratio (ϑ21) in transverse                        55

direction obtained by rules of mixture

4.6                          Ultimate load in Newton’s and elongation                                                      56

4.7                          Stress, Strain and Young’s modulus in longitudinal direction                        56

obtained by experimentation

4.8                          Young’s modulus in longitudinal direction obtained by simulation               57

4.9                          Shear Module’s (G12) calculated using rules of mixture                                 66

LIST OF FIGURES

Figure No.                                Name                                                               Page No.

1.1                             Different types of Composites materials                                                       7

1.2                             Classification of Natural Fibers                                                                     11

3.1                             Isostress and Isostrain Condition for Simple Unidirectional Composite       27

3.2.1                          Simple parallel model of unidirectional composite                                       27

3.2.2                          Simple series model of unidirectional composite                                          27

3.3                             Definition shear relative to the X1,X2Cartesian axis                                     29

3.4                             Raw jute                                                                                                         33

3.5                             Glass Tape                                                                                                      33

3.6                             Refined fibers ready to use                                                                             33

3.7                             Tensile Test Samples                                                                                      35

3.8                             Flexural Test Samples                                                                                     36

3.9                              Impact Test samples                                                                                       36

3.10                           Tensile Testing Machines in Unloaded Condition                                          38

3.11                           Tensile Testing Machine Performing Flexural Test                                        39

3.12                            Izod Impact Testing Machine                                                                         39

3.13                            Solid95 Element                                                                                             40

3.14                            Sample modeling of tensile samples in ANSYS                                            41

3.15                            Sample Analysis of Tensile Sample                                                               41

4.1                              Variation of the Flexural Modulus in Different Samples Obtained               45

By Experimentation (Three-Point-Bending Test)

4.2                              Variation of the Flexural Modulus of Composite obtained by                       47

Experimentation (Three-Point Bending Test) in Hybrids with Respect

to Pure Samples.

Figure No.                                Name                                                               Page No.

4.3                              Variation of the Flexural Modulus by varying the jute content                      48

in the pure matrix of Composite Obtained by Experimentation

(three-point bending test)

4.4                              Variation of the Flexural Modulus by Varying the Glass Content in the       48

Pure Matrix of Composite Obtained By Experimentation

(Three-Point-Bending Test)

4.5                              Variation of the Energy Absorbed in Joules by Different Samples                50

obtained by Experimentation (Izod impact testing)

4.6                             Variation of the Impact strength in joulesmm2 by Different Samples         50

Obtained experimentation (Izod impact testing)

4.7                              Variation of the Impact Strength of Composite obtained by                          51

Experimentation (Izod Impact testing) in Hybrids with Respect to

Pure Samples

4.8                              Variation of the Impact Strength by varying the jute content in the               52

pure matrix of Composite Obtained by Experimentation

(Izod Impact Strength test)

4.9                              Variation of the Impact Strength by varying the Glass content in the            53

pure matrix  of Composite Obtained by Experimentation

(Izod Impact Strength test)

4.10                            Young’s Modulus (E1) of Composite Obtained by Rules of Mixture,           58

Ansys and Experimentation

4.11                            Variation of Poisson’s ratio (ϑ12) in longitudinal direction                            59

4.12                            Variation of Poisson’s ratio (ϑ21) in Transverse direction                              59

4.13                            Variation of the Young’s Modulus (E1) of Composite Obtained by              61

Rules of Mixture, Ansys and Experimentation in Hybrids

With Respect to Pure Samples

Figure No.                                Name                                                               Page No.

4.14                          Variation of the Young’s Modulus (E1) by varying the jute content               62

in the pure matrix of Composite Obtained by Rule of Mixture,

Ansys and Experimentation.

4.15                           Variation of the Young’s Modulus (E1) by varying the glass content             63

in the pure matrix  of Composite Obtained by Rule of Mixture,

ANSYS and Experimentation.

4.16                           Variation of the Poisson’s ratio (ϑ12) of hybrid Composite Obtained            64

by rule of Mixture with respect pure sample of glass and jute.

4.17                           Variation of the Poisson’s ratio (ϑ21) of hybrid Composite Obtained            64

by rule of Mixture with respect pure sample of glass and jute.

4.18                           Variation of the Poisson’s ratio (ϑ12) by variation of jute content                  65

in the pure matrix Obtained by Rules of Mixture.

4.19                           Variation of the Poisson’s ratio (ϑ21) by variation of jute content                  66

in the pure matrix Obtained by Rules of Mixture.

4.20                           Variation of the Shear modulus (G12) by variation of fiber content in            67

pure matrix Obtained by Rules of Mixture.

4.21                          Variation of the Shear Modulus (G12) In Hybrids with Respect                      68

to the Pure Samples obtained by Rules of Mixture.

LIST OF SYMBOLS

Vf                                    Volume fraction of fiber

Vm                                    Volume fraction of matrix

E1                                    Young’s modulus in longitudinal direction

Et                                    Young’s modulus in transverse direction

ϑ12                                   Major Poisson ratio (relating to the lateral strain, ε2  when a stress

is applied in the longitudinal (X1) direction)

ϑ21                                   Minor Poisson ratio (relating to the strain in the (X1) direction

when a stress is applied in the (X2) direction)

G12                                    In-plane shear modulus